# Joint Stock Company

# “PIKALEVSKAYA SODA”

187600 Russia, Leningrad Region, Pikalevo, Spryamlennoe shosse 1

Phones: +7(495) 231-27-47 (ext. 2762), +7(495) 231-27-47 (ext. 2302),  +7(813) 664-39-82

QUALITY SPECIFICATION

POTASSIUM CARBONATE

|  | Calcinated | 1,5-hydrated |
| --- | --- | --- |
| Chemical parameters & Physical properties | Premium grade | Superior grade | 2nd grade and salt carbonate | 2nd grade improved |
| K2CO3 mass content, %, minimum | 99,3 | 99,3 | 94,0 | 97,0 |
| Sodium mass content (as Na2CO3), %, maximum | 0,25 | 0,25 | 3,2 | 2,0 |
| Chloride mass content (as Cl'), %, maximum | 0,01 | 0,01 | 1,0 | 0,5 |
| Sulphate mass content (as SO4"), %, maximum | 0,1 | 0,1 | 0,6 | 0,4 |
| Iron mass content (as Fe2O3), %, maximum | 0,001 | 0,001 | 0,005 | 0,001 |
| Aluminium mass content (as Al2O3), %, maximum | 0,06 | 0,06 | 0,8 | 0,4 |
| Chromium mass content (as Cr2O3), %, maximum | 0,0002 | 0,0004 | - | - |
| Insoluble residue mass content, %, maximum | 0,01 | 0,01 | 0,1 | 0,01 |
| Loss on ignition mass content (at t 500оC), %, maximum Granulometry, %: particle size – 0,16 mm particle size + 1,25 mm particle size + 1,6 mm | 0,5 no more > 10 no more > 5 0 | 0,5 no more > 10 no more > 5 0 | 20,0 | 18,5 |